國產疏伐木應用於桁架橋之研究

Application of Domestic Thinnings on the Trussed Bridge

研究生：林玉麗  Lin, Yu-Li

指導教授：葉民權  Yeh, Min-Chyuan

【摘要】

本研究之目的在探討台灣杉疏伐木作為結構用桁架樑系統之彎曲性質，以圓木型態組合成實大尺寸試材採用四點載重進行試驗，並依規範建造一步道橋，探討其可行性，同時利用空間桁架分析軟體，作華倫式平面桁架系統分析，評估橋樑受載重時桁架構材之應力及應變情形，與實驗結果進行比較，並依內政部營建署木構造建築物設計及施工技術規範，進行桁架樑之構材結構分析以及螺栓接合設計，另進行螺栓拉伸測試，模擬桁架樑構材節點之螺栓接合，進一步探討其接合性能。

三種台灣杉桁架樑系統彎曲試驗結果顯示，以跨距6 m直徑15 cm圓木之條件，其破壞時之最大彎曲載重值最高，為直徑12 cm圓木組成之桁架樑的1.7倍，及跨距4 m直徑12 cm圓木者之1.2倍。依規範活載重設計條件下，所測之變位量均未超過規定之最大彎曲變位量限制，且僅為所開發桁架系統規定之5-38%，同時設計活載重亦僅為破壞時之等效均布載重的13.9-23.9%。

螺栓接合拉伸試驗結果顯示，台灣杉圓木以單支螺栓接合之最小破壞拉伸力為設計值之7.3倍，雙支螺栓則為7.5倍，因此直徑1.588 cm之螺栓應用於本研究之桁架步道橋系統時，其強度性能遠超過於設計值而符合需求。

台灣杉圓木桁架橋依施工技術規範，進行各部位弦材之應力計算，在設計載重下各構材之應力值均未超過容許應力，桁架壓縮弦材設計值分別為容許應力之14-35%，拉伸弦材設計值則為容許應力之23-50%。透過應變片之量測結果，各構材之受力分布多與理論桁架計算相符，部分之差異應來自於桁架系統組裝作業的容許精準度。

所建造之6 m長步道橋于活載重二個月的期間，其潛變速率即呈穩定階段，且達6個月總潛變量之91%；瞬間之彈性變位僅為規範限制值之29%，在室外4個月期間構材含水率開始降至纖維飽和點以下，至6個月時尚未有耐久性的缺點發生。

【關鍵詞】疏伐木、桁架樑、步道橋、螺栓。

【Abstract】

The purpose of this study was to investigate the flexural properties of truss system fabricated with thinnings of Taiwania plantation. The four-point loading tests were performed for physical sizes of truss specimens assembled with round wood members. A pedestrian bridge was built based on the newly established building code to evaluate the feasibility of using thinnings as the structural members. The Warren plane truss systems subjected to the bridge design loads were analyzed by using the truss analysis software for force distribution and the results were compared to the experimental works. The structural member analysis and bolt connection design of the truss systems were performed following the code requirement, and the tension tests were also performed for the bolts used in the truss member connections.

The maximum bending capacity at failure of 6-m truss system fabricated with round wood of 15 cm in diameter is 1.7 times of that fabricated with round wood of 12 cm in diameter, and 1.2 times of 4-m truss system with 12 cm round wood members. The flexural deflection of the Taiwania truss system measured at the design live load conditions were 5-38% of design limitation, and the design live load is about 13.9-23.9% of maximum equivalent distributed load measured at rupture. The minimum tensile force  of the single-bolt joint with Taiwania round wood member is 7.3 times of allowable shearing stress calculated by the code procedure, and 7.5 times forthe double-bolt joint. It indicated that the 1.588 cm bolt can be satisfied in the application of trussed pedestrian bridge assemblies.

The stresses of the major chord members estimated based on the code specification with the design loads are all lower than the allowable stresses for Taiwania round wood. The compressive stresses of the chord members were 14-35% of allowable stresses, while the tensile stresses of the chord members were 23-50% of the allowable stresses. Based on the strain measurements, the stress for each chord member is close to the theoretical truss calculation results. Some deviations may come from the operation of truss system assemblies.

The creep behavior of 6-m pedestrian bridge was in steady stage after two months of live loads, and the flexural deflection reached to 91% of that measured after loaded for six months. The instantaneous elastic deflection at the center of the bridge subjected to live loads was 29% of limited deflection specified in the code. The moisture content of Taiwania round wood members were lower than fiber saturation point after four-months exposure. There is no any defects resulted due to decay or weathering action after the wood bridge built for six months.

【Key words】Thinning, Truss beam, Pedestrian bridge, Bolt.